## Slide 1: M4 & LPBF Parameters
17 materials · 21 October 2026
Notes: Overview of the extraction scope and the proposed model architecture. No measured data shown.

## Slide 2: Scope: two parameter sets pulled from 17 material workbooks
Source: shared NTU folder › Material Data › <material> › Excel workbook (one per material, 17 total)
Metal AM powder
WP1 · M1
LPBF-printed disc
WP1 · M2
Disc characterisation
WP2 · M4 (this update)
ICP + XRF
WP2 · M5 / M6
ML training set
WP3 · M7
LPBF parameters (how each disc was printed)
Laser power, scan speed, hatch spacing, layer thickness
Scan strategy, spot size, atmosphere, build-plate temperature
Derived: volumetric energy density (VED)
M4 results (what the printed disc looks like)
EDS: disc surface chemistry vs. nominal / powder
Micro-CT: porosity, relative density, defects
XRD: phases present, any texture or new phases

## Slide 3: LPBF fields extracted per material, normalised to common units
P
Laser power
W
v
Scan speed
mm/s
h
Hatch spacing
µm
t
Layer thickness
µm
—
Scan strategy
e.g. stripe, 67° rotation
d
Spot size
µm
—
Atmosphere / O₂
Ar / N₂, ppm
T
Plate preheat
°C
Derived metric
Volumetric energy density
E = P / (v · h · t)
J/mm³
Lets us compare print conditions across alloys on one axis
Checked against Micro-CT density in M4
Missing inputs flagged rather than assumed

## Slide 4: Model architecture: correcting loose-powder XRF towards ICP
INPUTS
Loose-powder XRF spectrum
Energy channels, repeat packings
Powder morphology
PSD (D10/D50/D90), shape, tap density
Omnian FP estimate
Baseline wt% per element
ENCODERS
1D CNN
Peak + background features
MLP
Morphology embedding
Pass-through
Physics prior
FUSION
Feature fusion
Concatenate + attention across inputs
HEAD
Residual correction
Δ wt% per element added to the FP estimate, with an uncertainty band
OUTPUT
Corrected composition
Target: ICP-level accuracy and precision
Supervision: ICP of powder and printed disc is the ground truth. LPBF discs, checked in M4 (EDS, Micro-CT, XRD), give homogeneous solid reference spectra.

## Slide 5: Where M4 and LPBF parameters plug into training
Ground truth
ICP on powder and on printed disc
M4 EDS / XRD confirm disc chemistry matches powder
LPBF parameters flag volatile-element loss (e.g. Mg, Zn)
Training data
2–3 loading protocols per alloy
~100 XRF repeats per protocol
Sieved sub-fractions to vary particle size
Validation
Hold out whole batches, not single scans
Test on unseen batches and powder CRMs
Per-element error and repeatability vs ICP

## Slide 6: Next steps
1. Extract
Pull M4 + LPBF fields from all 17 workbooks into one master table
2. Validate
Normalise units, compute VED, flag gaps and inconsistencies
3. Link to M5 / M6
Join disc data with ICP and XRF results per material
4. Feed WP3
Hand a clean, versioned dataset to Malvern's ML team
Discussion: confirm the 17 material names, the expected M4 fields, and the data owner for any gaps